## Slide 1: KJM 3110 Electrochemistry Chapter 14 Other interfaces
Most figures from the textbook we use for the course, via its web resources:

## Slide 2: Summary Ch. 13 The electrode interface
Interface
  Large capacitance
  Compact and diffuse adsorption layers
  Non-faradaic currents
  Adsorption
  Next chapter: Other interfaces
ionic conductor
metal

## Slide 3: Metallic and semiconducting electrodes
Metallic electrode:
  Working electrode is a metal (=is metallic (?))
  Always abundance of electrons
  Or rather: … Always abundance of electrons and states the electrons can be in.
Semiconducting electrode:
  Working electrode is a semiconductor (full valence band, empty conduction band)
  Not necessarily an abundance of electrons or states.

## Slide 4: Semiconductor electrodes - overview
Semiconductor
  Molecule → Lattice
  HOMO → Valence band
  LUMO → Conduction band
  Band gap
  Fermio level: (electro)chemical potential of electrons
  Work function: Energy to bring electrons to vacuum
n-type semiconductor
  Donor-doped n = [e-] = [D+]
  Electrons e- in the conduction band
p-type semiconductor
  Acceptor-doped p = [h+] = [A-]
  Electron holes h+ in the valence band

## Slide 5: n-type electrode – a closer look
Bulk of n-type semiconductor:
n ≈ [D+]
Fermi (energy) level near conduction band
Interface:
Adsorption of anions in Helmholtz layer
compensated by
positive space charge in the semiconductor
by
depletion of electrons
excess of holes
Band bending:
Cause: Adsorption of one of the ions
Shape: Boltzmann distribution, Poisson
-
-
-
-
-
-
-
-

## Slide 6: Adsorption vs redox
In the previous slide, and in the textbook in general, the semiconductor charge and energy levels are affected by selective adsorption of ions.
Another possibility is that the electrolyte-electrode interface has a potential (Fermi level) determined by a redox reaction.
Charge flows into the electrode to align its Fermi level with the redox reaction.
But the level at the interface remains pinned. Band bending.

## Slide 7: Exercise
How do the bands look before contact with the electrolyte?
Based on your memory and understanding, populate the top figure with ions, electrons, and holes
Populate the bottom figure with ions, electrons, and holes
How could we force the bands flat?
What is the flat-band potential?
Try to populate the valence bands with electrons instead of holes

## Slide 8: Photoelectrochemical (PEC) cell
n-type photoanode or p-type photocathode
Suitable bandgap
Charge separation
Photoanode

## Slide 9: PEC water splitting, artificial photosynthesis
Low efficiencies
Photocorrosion of electrodes
Cathode traditionally a noble (platinum group) metal
  Research: Non-noble metals, oxides. Enzymes
Sunlight cannot drive the reaction alone, just assist it
  Research: Combine photoanode and photocathode. Combine PV and PEC.
Reduce CO2 instead of H2O
Solid-state electrolyte instead of aqueous

## Slide 10: Artificial photosynthesis
Fujitsu Journal

## Slide 11: The following slides about “ITIES” are not curriculum…

## Slide 12: Interface between two immiscible electrolyte solutions (ITIES)
Aqueous vs organic liquids
Use of bipotentiostat

## Slide 13: Redox scales – SHE and ferrocene (C5H5)2Fe – for ITIES

## Slide 14: ITIES ion and electron transfers
Proton
Electron

## Slide 15: ITIES combined proton and electron transfers

## Slide 16: Phospholipid….
Zwitterion
Not curriculum

## Slide 17: From here we are back at curriculum again:
Electrolyte – insulator interfaces

## Slide 18: Electrokinetic phenomena
Electrical double layers can initiate movement and this is the source of the adjective electrokinetic [“electrically generated motion”] used to describe these phenomena.
No direct relationship to “electrode kinetics”, despite similar name
Electrolyte – insulator interface
No electrical current across
But double layers form
Scales with interface area: Porous materials, suspensions, etc.
Silica:
  Terminating covalent O, denoted as >Si=O
  H2O adsorb
  Protolyses weakly (Silica is weakly acidic)
Glass
  Ionic alkali cations compensated by ionic terminating oxygen
  Reduces acidity
Adsorption of cations like Al3+ may reverse the charge

## Slide 19: Charged particles and walls
Silica and other materials with double layers can be mobile particles or stationary walls
Nernst, Stern, and zeta potentials
Shearing planes = slipping planes
Electrical field moves net charge and drags water

## Slide 20: Electroosmotic drag
Diffuse layer is net charged and mobile outside of the slip plane
Electrical field yields velocity profile of the liquid phase

## Slide 21: Electroosmotic drag
Friction between the positive double layer and the solution volume
Volume rate v (m3/s)
Field X, radius R, viscosity η
Zeta potential ζ at the slip plane
  (zeta is ζ in the font set, not like in the formula in the textbook)
  Similar to Helmholtz potential φH
  Around -150 mV for glass, higher for silica
Electroosmotic flow is laminar, but it does not have the quadratic dependence of
velocity on radius, as described on pages 161-162, that is seen in Poiseuille (laminar) flow. This is because electro-osmotic flow is not pressure-driven; instead, it is induced by friction from the motion of the field-driven sleeve. Thus the velocity profile is as shown in the Figure: it is uniform apart from within the narrow double-layer region.

## Slide 22: Water drag in PEMs is called electroosmotic, but is a bit special…
Polymer is net negative by sulfonate –R-SO3- terminating groups
Water phase is net positive by H3O+ ions
Electroosmotic drag on water phase in electrical field
H3O+ may be seen as positive particle dragging 5-6 coordinated water molecules

## Slide 23: Electroosmotic drag
Electroosmotic flow by voltage or current
Electroosmotic pressure by voltage or current
Streaming potential or current by flow or pressure
Universality, e.g.
Lars Onsager reciprocal relations
Irreversible thermodynamics
Nobel prize 1968
Lars Onsager
Lars Onsager

## Slide 24: Ch. 14 Other interfaces - Summary