## Slide 1
KJM3110 Electrochemistry
Expansion of Ch 5 on Batteries
Truls Norby
(thanks to prof. Ola Nilsen for many inputs and figures)
Some slides are integrated from those in Ch 5 so as to contain all on batteries here

## Slide 2: Storage
Battery: Chemistry
Ultracapacitor: Chemistry + electrode interface
Supercapacitor: Electrode interface
Capacitor: Dielectric

## Slide 3: Overview: Batteries, fuel cells, and electrolysers
Primary batteries
  Factory charged
  Single discharge
Secondary batteries - accumulators
  Rechargeable
  Multiple discharges and recharges
  All chemical energy stored
“Ternary batteries” – fuel cells
  Fuel continuously supplied from external source
Electrolysers
  Reversed fuel cells
  Fuel generated continuously and stored externally

## Slide 4: Battery key features
Positive and negative electrodes
Positrode and negatrode
Cathode and anode
Cell voltage terms
  Nominal voltage = OCV fully charged
  Cut-off voltage
  Operational voltage range
  Null voltage?
Capacity (amount of charge)
  Coulomb, C = A s
  1 A h = 3600 A s = 3600 C
Energy
  J = W s = A s V
  U = 4 V
  Typical car battery stacks: 20-80 kWh
  Energy density (volumetric or gravimetric)
Power
  W or kW
  W = A V
  Typical cars: 100-400 kW
  Ustack = 400 V → Istack = 25–100 A

## Slide 5: Primary batteries
Volta pile
Daniell cell
Leclanché wet cell with NH4Cl(aq)
Dry cell
  NH4Cl + ZnCl2 paste
  C powder composite cathode
Zn + 2MnO2  2ZnO*Mn2O3 1.5 V

## Slide 6
The zinc-carbon battery (dry cell)

## Slide 7
Alkaline battery – in principle…
Anode (-)
Zn + 2OH-  ZnO + H2O + 2e–
Cathode(+)
2MnO2 + H2O + 2e –  Mn2O3 + 2OH-
 Mn3O4
Electrolyte
KOH
Zn + 2MnO2  ZnO*Mn2O3 1.5 V

## Slide 8
Alkaline battery – in reality

## Slide 9: Alkaline batteries
Inversed design…
Other alkaline positrodes
Air battery

## Slide 10
Pb battery
Anode (-)
Pb + HSO4 –  PbSO4 + H+ + 2e–
Cathode(+)
PbO2 + 3H+ + HSO4 – + 2e –  PbSO4 + 2H2O
Electrolyte
H2SO4
Pb + PbO2 + 2H2SO4  2PbSO4 + 2H2O 2.0 V

## Slide 11: Secondary (rechargeable) batteries (accumulators)
Most widespread: Lead-acid battery.
Repeat from Ch. 3:

## Slide 12: Lead acid battery

## Slide 13: Lead acid batteries: Extraneous reactions
In modern, sealed batteries, diffusion of O2 + reaction 5.24 replenishes the water.

## Slide 14
NiCd battery
Anode (-)
Cd + 2OH–  Cd(OH)2 + 2e–
Cathode(+)
2NiO(OH) + 2H2O + 2e –  2Ni(OH)2 + OH-
Electrolyte
KOH
Cd + 2NiO(OH) + 2H2O  2Ni(OH)2 + Cd(OH)2 1.2 V

## Slide 15
NiCd battery

## Slide 16
NiMH battery
Anode (-)
OH- + MH  M + H2O + e –
Cathode(+)
NiO(OH) + H2O + e–  Ni(OH)2 + OH-
Electrolyte
KOH
NiO(OH) + MH  Ni(OH)2 + M 1.3 V
M = AB5, AB2 A= Ce, Nd, Pr, Gd, Y, La B= Ni, Co, Al, Ti, Zr, Si

## Slide 17
NiMH battery

## Slide 18: Na-S battery
Exercise: What is the total reaction and Gibbs expression?

## Slide 19: Redox flow battery
What are the electrodes?
What goes on in the membrane?

## Slide 20
Role of electrolyte
Both NiCd and NiMH batteries require some volume for the electrolyte, as material is moved from the electrodes into the electrolyte, and vice versa.
Would it not be better if the ionic charge could merely travel from within the anode, through the electrolyte, into the cathode?
And back. The rocking chair battery.
The electrolyte could then be reduced to a simple ionic conductor.
This is exactly the idea behind the Li+ ion battery

## Slide 21: Li ion batteries

## Slide 22
Li-battery – The beginning
The concept of rechargeable lithium batteries was first demonstrated with a transition metal sulfide TiS2 as the cathode, metallic lithium as the anode, and a nonaqueous electrolyte.
Li
2 V
Ti4+ -> Ti3+

## Slide 23: Modern Li-ion batteries
M. Stanley Whittingham (1941-) proposed the first Li ion battery in the 1970s.
John B. Goodenough (1922-) proposed today’s cathode materials.

## Slide 24
Charge
Discharge
LiCoO2
LiMn2O4
LiFePO4
Graphite
Li battery
4 V

## Slide 25: Li-ion batteries
Positrode: Simple
or more realistic
Negatrode:
Copyright 2013, ACS
The electrolyte used in most lithium-ion cells is a solution of LiClO4 or LiAsF6 in organic carbonates, absorbed in microporous polyolefin separator.

## Slide 26: Li ion battery electrolytes

## Slide 27: Requirements of the electrolyte
Conduct Li+ ions
Not react with electrodes
Not oxidised or reduced (electrolysed) at the electrodes
  Must tolerate > 4 V
  Chemical redox stability
  Band gap
Harder during charge than discharge

## Slide 28: Liquid Li ion conducting electrolytes
Aqueous solutions cannot withstand 4 V
  Water would be electrolysed (gas evolution during charge)
  Li metal at the anode reacts with water
Li+ ion electrolytes must be non-aqueous
  Li salts
    E.g. LiPF6, LiBH4, LiClO4
  dissolved in liquid organic solvents
    e.g. ethylene carbonate
    possibly embedded in solid composites with
    Polyethylene oxide (PEO) or other polymers of high molecular weight
    Porous ceramics
Conductivity typically 0.01 S/cm, increasing with temperature
http://www.sci.osaka-u.ac.jp

## Slide 29: Solid Li+ ion electrolytes
Incombustible in air in case of leakage
Can be thinner than liquids and polymers
Reduced chance of whisker short-circuits
Challenges of band gap and Li+ diffusion
Li3xLa3/2-xTiO3 perovskites
Li7La3Zr2O12 garnets
Li2S

## Slide 30: Li3xLa2/3-xTiO3 perovskite
A.I. Ruiz et al., Solid State Ionics, 112 (1998) 291–297

## Slide 31: Li7La3Zr2O12 (LLZO) garnet
Stabilised in the cubic form by high temperature or doping, e.g. with Al3+ substituting Li+ or Nb5+ substituting Zr4+
8-coordinated La3+
6-coordinated Zr4+
Li1 and Li2 sites
Partial occupancy 7/9 of Li sites facilitates self-diffusion

## Slide 32: Li2S
Antifluorite structure
Diffusion by jumps between regular tetrahedral and interstitial octahedral sites
Doping with higher-valent cations: P5+, Ge4+
  Increases concentration of Li vacancies
May use S/Li2S as cathode
  Composite with e.g. graphite or graphene

## Slide 33: Li ion battery anodes

## Slide 34
Metallic Li anodes
Metallic Li anode is a practically good anode to work with under production, but what can happen during:
Rapid charging?
Rupture?

## Slide 35
LiC6
Direct reaction of well crystalline graphite and metallic Li will result in LiC6, passing through (LiC12, LiC18 …).
Can intercalate Li up to LiC2, however, this is unstable:
3 LiC2 -> LiC6 + 2Li.
E0 for the anode is raised 0.1-0.2 V to the LiC6/Li+ as compared to Li/Li+.
Question: What implications does this give?
What is lost in electrochemical capacity is gained in safety.
Why is electroplating during charging avoided?
Exercise: Why does the overall capacity vary with potential? How do you calculate the energy capacity from potential and… something more…?

## Slide 36
LiC6
Direct reaction of well crystalline graphite and metallic Li will result in LiC6, passing through (LiC12, LiC18 …).
Exercise C: Regard the different stages of intercalation in graphite and consider these as individual phases. Use the Gibbs phase rule to argue that you would expect to observe steps in the potentiometric diagram rather than a slope.
Exercise D: How would the potentiometric graph appear if the material shows complete solid solubility with respect to Li+ content?

## Slide 37: Si anodes
Using micro- and nanoscopic Si keeps structure porous and allows Li to intercalate without changing macroscopic dimensions
Si on C backbone
Porous Si
Norwegian Cenate AS (centrifugal nanotechnology) produces nano Si for battery anodes

## Slide 38: Li ion battery cathodes (Brief introduction – much more materials chemistry in other courses (KJM-MENA 3120, MENA 3201)

## Slide 39
Mainly two classes of Li cathode materials:
(1) Layered compounds with an anion close-packed or almost close-packed lattice in which alternate layers between the anion sheets are occupied by a redox-active transition metal and lithium then inserts itself into the essentially empty remaining layers.
Exemplified by first LiTiS2, followed by LiCoO2, LiNi1-yCoyO2, and today LiNiyMnyCo1-2yO2. The spinels may be considered as a special case
where the transition-metal cations are ordered in all the layers.
This group has rather compact lattices, which is an inherent advantage in energy stored per unit of volume.
Two classes of Li cathode materials

## Slide 40
Mainly two classes of Li cathode materials:
(2) More open structures, like many of the vanadium oxides, the tunnel compounds of manganese dioxide, and most recently the transition-metal phosphates, such as the olivine LiFePO4.
This group has potentially lower cost .
Two classes of Li cathode materials

## Slide 41: SEI and SPI
Solid electrolyte interphase (SEI)
  Forms by reduction of electrolyte at the negatrode
  Supports migration and diffusion of Li+ ions
Solid permeable interface (SPI)
  At the positrode

## Slide 42: EIS on Li ion batteries
Relectrolyte, Rgb, Rct, RSEI, Qwarburg, chemical

## Slide 43: Charge-discharge curves
The cell voltage can be recorded as a function of many parameters that measure the discharge of the battery
Time
Capacity or specific capacity
  Steady state
  Charge or charge/g
Composition
  Li content
  Finite rate
  Monitored with in-situ

## Slide 44: Coin cells for application and research
Commercial
Laboratory
  Made in inert atmosphere (glove-box)
  Prevents air-intrusion
  Allows electrochemical and performance characterisation + in-situ measurements
® Jan Petter Mæhlen

## Slide 45: Battery stacks
Typically 100 cells stacked in series to a module of 400 V
Several modules in parallel
Control electronics for e.g. 12 cell subunits

## Slide 46: Safety aspects of high-power Li-ion batteries
High voltage
  Series connected, e,g, 100 x 4 V = 400 V → lethal
  Rigid insulation and warning/shut-off systems
High currents
  Resistance may give overheating → fire
    Monitor overpotentials
Internal short-circuit
  Whiskers
  Runaway reactions between cathode and anode components → fire
  Individual cell(s) control
Leakage
  High redox stability (4 V) of materials, but not towards O2 or H2O
  Anode (e.g. C + Li) combust with O2 and Li reacts with H2O
    Intercalation in e.g. C or Si prevents explosive speeds
  Liquid electrolyte solvents (e.g. PEO) combust with O2
  Mechanical integrity during charge/discharge, vibrations, shock, collision